Balsan 
Balsan moquette
2 Corbilly
F-36330 ARTHON
www.balsan.com
Monday 14 March 2022 

BALSAN - MATRIX 

The selected type of floor covering is Textured loop pile carpet tile - CYP Colorpoint Technology backing, in 50x50cm removeable, loose-lay tiles, belonging to the Tile range made by BALSAN or else an equivalent. 

The carpet complies with FIRE Bfl-s1 - affixed on concrete. 

It will provide impact sound insulation of ΔLw 28 dB (NF EN ISO 140-8) and airborne sound insulation of αω 0.35 (NF EN ISO 11654). 

It will be made from 100% solution dyed nylon - 75% recycled with a total weight of 4065 g/m² - 119.9 oz/sq yd (NF ISO 8543) and fibre weight of 500 g/m² - 14.7 oz/sq yd, with 220 g/m² - 6.5 oz/sq yd pile above backing, and a total thickness 9.2 mm (NF ISO 1765). 

It will have permanent antistatic treatment. 

The Tile carpet will have PRODIS accreditation, number N° D47E97FA. 

Total airborne VOC emissions at 28 days (NF EN 16000) for the selected flooring will be less than < 100 µg/m³, rated as A+ for health purposes (the highest rating). 

CHARACTERISTICS AND LAYING

Fiber Weight (g/m²) - (oz/sq yd) - NF ISO 8543 : 500 - 14.7
Surface Pile Weight (g/m²) - (oz/sq yd) - NF ISO 8543 : 220 - 6.5
Total Weight (g/m²) - (oz/sq yd) - NF ISO 8543 : 4065 - 119.9
Total Height (mm) - (in) - NF ISO 1765 : 9.2 - 0.362
Pile Height (mm) - (in) - NF ISO 1766 : 3.4 - 0.134
Tightening (points) - (SPI) - NF ISO 1763 : 38 - 9.7
Density (p/m²) - (Tufts) - NF ISO 1763 : 150100 - 495738721

Laying and maintenance should comply with the recommendations on our website www.balsan.com and available from our Sales Department on
+33 (0) 2.54.29.16.00.